Fabrication, Characterization, and Measurement of Some Physicochemical

Properties of ZnO Nanofluid

Majid Moosavi, a Elaheh K. Goharshadi, a,b* and Abbas Yousefic

a Dept. of Chemistry, Ferdowsi University of Mashhad, Mashhad 91779, Iran

b Center of Nano Research, Ferdowsi University of Mashhad, Iran

c Pare-Taavous Research Institute, Mashhad, Iran

E-mail: gohari@ferdowsi.um.ac.ir

Nanofluids are a new kind of fluids containing a very small quantity of nanoparticles that are uniformly and stably suspended in a liquid. Choi [1] coined the term “nanofluids” for this new class of solid/liquid suspensions, developed primarily for heat transfer applications.

ZnO nanofluids have been prepared by dispersing ZnO nanoparticles in the ethylene glycol (EG) and glycerol as base fluids. Ammonium citrate, as a dispersant, has been used to improve the dispersion of nanoparticles and suppressing formation of particle clusters to obtain stable suspensions.

Undoubtedly, the most important property of nanofluids is thermal conductivity. A large number of investigations have been reported for thermal conductivity of different nanofluids [2-4] but just a little work has been made on other properties such as viscosity [5,6] and surface tension of nanofluids. The use of nanofluids in other applications is under developing, for example, some nanofluids such as TiO2 and ZnO can be also used as antibacterial media [7,8].

The thermal conductivity of ZnO nanofluids have been measured as a function of the volume fraction and temperature. The thermal conductivity of ZnO/EG and ZnO/glycerol nanofluids increases nonlinearly up to 10.5% and 7.2%, respectively, as the volume fraction of particles increases up to 3 vol.%. The thermal conductivity of a ZnO nanofluid increases nonlinearly with increasing the temperature at a constant volume fraction of nanoparticles.

For the first time, we have measured the viscosity and surface tension of ZnO nanofluids. The viscosity ratio of nanofluids increases with increasing concentration and decreasing the temperature. The surface tension ratio of suspensions containing solid particles increases with increasing the volume fraction of the solid particles.

The experimental data for thermal conductivity and viscosity have been compared with some existing theoretical models.

Keywords: Nanofluid; Thermal conductivity; Viscosity; Surface tension; Zinc oxide

References

[1]. U. S. Choi, in “Developments and Applications of Non-Newtonian Flows” (D. A. Siginer and H. P. Wang, Eds.) FED Vol. 231/MD Vol. 66, p. 99. American Society of Mechanical Engineers, New York, 1995.

[2]. Y. Xuan, Q. Li, Int. J. Heat Fluid Flow 21, 58 (2000).

[3]. M. S. Liu, M. C. C. Lin, I. T. Huang, C. C. Wang, Chem. Eng. Thechnol. 29, 72 (2006).

[4]. M. Chopkar, P. K. Das, I. Manna, Scripta Materialia 55, 549 (2006).

[5]. R. Prasher, D. Song, and J. Wang, P. Phelan, Appl. Phys. Lett. 89, 133108 (2006).

[6]. Y. He, Y. Jin, H. Chen, Y. Ding, D. Cang, H. Lu, Int J. Heat &  Mass Transfer 50, 2272 (2007).

[7]. L. Zhang, Y. Jiang, Y. Ding, M. Povey, and D. York, J. Nanoparticle Research 9, 479 (2007).

[8]. K. Ghule, A. V. Ghule, B. J. Chen, and Y. C. Ling, Green Chem. 8, 1034 (2006).