Prediction of Excess Thermodynamic Functions and Activity Coefficients of Some Polymeric Liquid Mixtures Using a Simple Equation of State

Elaheh. K. Goharshadi, * Maryam Abareshi, Ali R. Berenji,  Maryam Imani, 
Fahmieh Razghandi, and Rayhneh Rahimi-Zarei

Dept. of Chemistry, Ferdowsi University of Mashhad, Mashhad 91779, Iran

Email: gohai@ferdowsi.um.ac.ir

Introduction

The topic of this study, excess thermodynamic properties of the binary mixtures, is one of the most interesting phenomena in molecular physics. They provide us information to understand the observed properties of the mixtures from the point of view of microscopic interactions [1]. Excess thermodynamic properties of mixtures provide insight into the molecular interactions between the various components and can be used for the development of molecular models describing the thermodynamic behavior of mixtures [2]. From a practical point of view, the excess molar volumes are useful for the design of mixing and storage tanks and transport equipments [3].

This study was undertaken to investigate the excess thermodynamic properties and activity coefficients of four polymer mixtures and blends consist of  poly (ethylene glycol methyl ether)-350 (PEGME-350) +  poly (ethylene glycol)-200 (PEG-200), poly(propylene glycol)-425 (PPG- 425)+PEGME-350(2), PEGME-350 + PEG-600, and PEG-200 + PPG-400 using the GMA EoS [4].

Theoretical Section

A simple equation of state (EoS) has been derived for liquids by Goharshadi et al. [4] (Goharshadi-Morsali-Abbaspour "GMA EoS"). It has been used to calculate the different thermodynamic and volumetric properties such as density, isobaric expansion coefficient, and isothermal compressibility for a wide range of fluids including polar, nonpolar, and hydrogen-bonded fluids [4-7]. The GMA equation of state has been also applied for calculating the thermodynamics properties of liquid mixtures [8-10]. The equation of state is based on the average potential energy and is given as:

(1)

where Z, Vm , and  are compressibility factor, molar volume, and molar density, respectively.

The intercept and slope of this equation depend on temperature via the equations:

(2)

(3)

where Ao - A2 and Bo - B2 are constants. To use the EoS for a liquid, the A and B parameters must be known. To find these parameters, we may plot (2Z−1)V3m against ρ for different isotherms. The slope and intercept of the straight lines can be fitted with Eqs. (2) and (3) from which Ao−A2 and Bo−B2 can be found.

The density based on GMA EoS can be calculated by the following equation:

(4)

The excess volume, VE, excess Gibbs energy,GE, excess enthalpy, HE, excess entropy, SE, excess internal energy, UE, and excess Helmholtz energy, AE, can be calculated using Eqs.5 to 10, respectively.

(5)                                                                                                                                                                    	             (6)

(7)

(8)                                                                                                                                           						                        (9)

(10)

The activity coefficient,, of a component in a binary mixture can be calculated by the following equation:

(11)

Results and Discussion

In this work, we have calculated excess thermodynamic properties such as excess molar Gibbs free energy, excess molar enthalpy, excess molar entropy, excess molar internal energy, and excess molar Helmholtz free energy of some binary mixtures at various temperatures, pressures, and compositions. Furthermore, the activity coefficients of polymeric mixtures have been calculated using this equation of state. A wide comparison with experimental data has been made for each thermodynamic property. The values of statistical parameters between experimental and calculated properties show the ability of this equation of state in reproducing and predicting of excess thermodynamic functions and activity coefficient for studied mixtures.

Typical graph for excess molar Gibbs energy for mixture of PPG-425 + PEGME-350 at 298.15 K and different pressures have been given in Fig. 1. Since PPG has specific interaction with PEGME due to the hydrogen bond, the values of excess molar enthalpy and excess molar entropy are negative at different pressures. The excess molar Gibbs energy was found to vary from negative to positive as increasing the mole fraction of PPG-425. The sign of excess molar Gibbs energy depends on the magnitude of excess molar enthalpy and excess molar entropy. In fact, liquid-liquid phase separation in polymer blend systems occurs through a competition between the enthalpy and the entropy of mixing. Figure 3 shows that the enthalpic effects arising from attractive forces are more important than the entropic ones in PPG-rich blend

Fig. 1. Experimental (symbols) and calculated (solid lines) excess molar Gibbs energy for PPG (1) + PEGME (2) versus mole fraction (a) at 298.15 K for different pressures.

Keyword: Excess thermodynamic functions, GMA equation of state, activity coefficient

References

[1] M. Koyuncu, A. Demirtas, and R. Ogul, Fluid Phase Equilib. 193, 87 (2002).

[2] M. Kwaterski, E. N. Rezanova, and R.N. Lichtenthaler, Fluid Phase Equilib. 237, 170 (2005).

[3] E. Kovacs, K. Aim, and J. Lineka, J. Chem. Thermodyn. 33, 33 (2001).

[4] E. K. Goharshadi, A. Morsali, and M. Abbaspour, Fluid Phase Equilib. 230, 170 (2005).

[5]  E. K. Goharshadi and A. R. Berenji, J. Nucl. Mat. 348, 40 (2006).

[6] M. Moosavi and E. K. Goharshadi, Int. J. Thermophys. 27, 1515 (2006).

[7] E. K. Goharshadi and F. Moosavi, Int. J. Refrig. 30, 377 (2007).

[8] E. K. Goharshadi and M. Moosavi, Ind. Eng. Chem. Res. 44, 6973 (2005).

[9] E. K. Goharshadi and M. Moosavi, Thermochim. Acta 64, 447 (2006).

[10] A. R. Berenji and E. K. Goharshadi, Polymer 47, 4726 (2006).