# MEASUREMENT AND PREDICTION OF RESIDUAL STRESS GENERATED BY LOCAL COMPRESSION

A.H. Mahmoudi, S. Hadidi-Moud, C.E. Truman and D.J. Smith.

Department of Mechanical Engineering

University of Bristol, UK, BS8 1TR

1. SUMMARY

In order to assess the effect of a residual stress field on the fracture behaviour of materials, a well-defined residual stress field, with known characteristics, such as triaxiality, must be generated in a controllable and reproducible manner. In this paper local compression, or punching, is used to introduce a residual stress field into a cracked plate, and the resulting residual stress field determined using Finite Element Analysis (FEA). However, great care must be taken using this approach, as it is well known that the elastic stress field created by a circular, flat-ended punch contains a stress singularity at the edge of the indenter. It is therefore imperative that, where possible, FE simulations are validated against analytical solutions to ensure confidence in the results. However, there are no analytical solutions for these residual stress fields. FE results for indentation of an elastic half-space are compared to analytical solutions. Results are then presented for the elastic stress field created by punching a finite sized block of material, of dimensions representative of a material test specimen, and the deviations from the half-space results are highlighted. The analysis is then extended into the elasto-plastic regime and the residual stress fields generated for these two geometries after the punching process are given. The residual stress field is measured in the finite sized specimen using deep hole drilling (DHD) and incremental centre hole drilling (ICHD) and compared to the FE predictions. Finally, local compression is applied to a specimen containing a crack. A parametric study is undertaken which examines the influence of the punching tool radius and punching position – relative to the crack tip – on the resulting residual stress field.

2. INTRODUCTION

In this paper, ‘local compression’ (LC) is used to denote the surface compression of different specimens using punching tools. LC has previously been used for several purposes. For instance, it has been used to relax residual stresses resulting from thermal or mechanical loads, such as those developed by welding. LC has also been used to examine material properties. In addition to frequently employed spherical or conical indenters [1], flat-ended rigid punches [2] have been employed in hardness tests on materials. When used to relieve residual stresses created by the welding process, standard procedures [3,4] suggest that the application of LC using flat-ended punches is often sufficient to reduce the welding residual stresses to low and uniform levels and results in the growth of straight fatigue precracks [1-2].

The punching tool will be a circular, cylindrical, flat punch. The surface pressure generated by such an indenter is well-known when the indented material has dimensions large relative to the punching tool and when no material yielding occurs. In other words, solutions exist for the elastic indentation of a half-space for the case of plane strain and axi-symmetry [1]. Nepershin [5] studied analytically the indentation of a flat punch into a rigid-plastic half-space using slip line fields. Sneddon [6,7] presented expressions for the interior elastic stress field produced in an elastic half-space when it was deformed by a rigid flat punch. There are limited studies on the stress field produced by a flat punch in finite-sized specimens. Lee and Kobayashi [8] predicted the load-displacement relationship and stress distribution.

In this work, LC is used to produce a residual stress field with well-defined characteristics. This enabled a consistent method of creating residual stress fields in specimens which would allow a study of the interaction between residual stress fields and applied loading. This interaction is of great importance in assessing the integrity of structural component containing cracks. In previous research, Almer et al [9] used a radial cold expansion method to produce residual stresses in front of the crack-tip in compact tension C(T) specimens. Ogeman [10] also used a coining process around a hole to introduce residual stresses. Hill [11] has used the LC technique to introduce residual stresses in single edge notch bend specimens.

In this work FE simulations were performed to determine the loading stresses in an elastic half-space in order to benchmark the FE simulation against the known analytical solution. The FE analysis was then extended to a) predict the residual stress field generated when the material was allowed to plastically deform and b) extend the analysis to finite dimensioned specimens, of sizes comparable to standard laboratory test specimens. The residual stress field in an aluminium plate was then measured experimentally using deep hole drilling (DHD) [12] and incremental centre hole drilling (ICHD) and results compared with the FE predictions. Finally, the residual stress field generated in a cracked C(T) specimen by LC was determined and a parametric study undertaken to examine the influence of punching tool radius and punching position, relative to the crack tip, on the characteristics of the residual stress field.

3. ELASTIC LOADING

## Half-space

No analytical solution exists for the residual stress field produced by a flat-ended punch. Therefore the elastic stresses created by a punch are examined under load in order to verify FE results against known analytical results. Although the residual stress field will eventually be introduced into specimens using two punching tools, one on either side of the specimen, a single punch is initially modelled to allow comparison with the analytical solution and provide confidence in the modelling procedure. The commercial code ABAQUS was used to perform the FE analyses [13]. A linear elastic analysis was undertaken, and to ensure half-space results were generated, the dimensions of the block were made

Figure1. Comparison of analytical and FE stress distributions, Z=0 (a) on the surface (b) along r=a

greater than about five punch diameters. The pressure distribution for axi-symmetric indentation of an elastic-half space by a rigid, flat punch is given as [1]:

(1)

where P is the pressure distribution on the surface, F is applied force, 2a is the diameter of the punch and r is the radial coordinate which is the distance the from the punch axis.

Fig. 1(a) shows the normalised surface pressure distribution as a function of the normalised radial coordinate. Fig. 1(b) shows the normalised stress, , as a function of the normalised depth coordinate, z. Good agreement is evident between the analytical solution and finite element results.  The finite element results correctly predicted the singular pressure around the edges of the punch, as given by equation (1). Approximately 8000 axi-symmetric elements were used in the FE model.

Figure2. Influence of remote boundaries on the stress field. (a) on the surface, Z=0 (b) along r=a

## Finite Sized Plate

It is useful to examine the perturbation on the stress field (as compared to the half-space solution) induced during LC caused by the presence of external boundaries. To enable this, a FE analysis of a plate of dimension 60*60*15 mm being indented by a 25 mm diameter punch was undertaken. These dimensions were chosen to be consistent with the laboratory specimens which would eventually be fabricated. A full three-dimensional FE analysis was undertaken using approximately 8000 8-node 3D elements. To assist in assessing the influence of remote boundaries on the elastic stress field created by punching, results are displayed in Fig. 2(a) and 2(b) which correspond to Fig. 1(a) and 1(b). It can be seen that the presence of boundaries increase the magnitude of the surface pressure and decrease the magnitude of the stress  along the line r=a.

## 4. THE RESIDUAL STRESS FIELD CREATED BY LOCAL COMPRESSION

Half-space

If yielding occurs during the loading phase, a residual stress field will remain upon removal of the load. As laboratory specimens for experimental tests were fabricated from aluminium alloy AL 2650, the material properties for this material were used in the FE simulations. Al 2650 has a modulus of elasticity of 72 GPa, a Poisson ratio of 0.33, and a yield strength of 427 MPa. A series of simulations using these material properties were carried out in the same sequence as section 3. An elasto-plastic material model was used to determine the generation of residual stresses firstly in a half-space. In-plane residual stresses through part of the thickness (up to z/a=3) of the half-space are shown in Fig. 3 for three different levels of penetration. During the simulations compressive loading was applied and increased until a prescribed level of indentation was introduced into the surface. After plastic deformation, the load was

removed and the resulting residual stress field determined. Three different displacements were applied to the rigid punching tools and the results in Fig. 3 indicate a tensile residual stress for Z/a=0.2 below the punch and then compressive residual stress deep inside the body. These results are similar to the results of Lee and Kobayashi [8] for a thick plate under local compression using a flat punch.

Uncracked plates

LC was then employed to generate a residual stress field in 60*60*15mm aluminum plates. In anticipation of the experimental procedure, LC was applied to both sides of these specimens using two punching tools.  Again, the analysis procedure consisted of applying a load, which resulted in yielding of the plate and then removal of the load to produce a residual stress field.

The analysis was performed under displacement control and the input displacement was adjusted to obtain a final reduction in thickness after removal of the punching tool equal to 1.6% of the specimen thickness. The amount of indentation was chosen based on previous work by Meith et al [11] who reported the effects of indentation on apparent fracture toughness. FE analysis was carried out using an elastic-plastic material model and a non-linear, large strain formulation. Distributions of residual stress through the thickness of the plate for two different material models, isotropic and combined hardening, are shown in Fig. 4.

The residual stress field was measured experimentally using the deep hole drilling (DHD) method [12] with a 1.5mm diameter reference hole and a 5mm-trepanned core. The incremental centre hole drilling (ICHD) technique was used on both sides of the specimen. Both measurements were performed in the centre of the punching imprint. The FE predictions and the measurements both illustrated compressive residual stresses through the thickness of the specimen.  This differed from those produced in a half-space where the residual stresses on the surface were tensile. It can be seen that the FE simulations predicted a greater level of compressive residual stress than the measurements.

Combined hardening data that more accurately described the material behaviour during compressive loading, obtained from Garcia-Granada [14], were used in the FE analysis. The residual stress distribution using the combined hardening material model was closer to the experimental results. The contact behaviour of the punch in all simulations was frictionless. The difference in measurement and FE results may be explained by the choice of element type and the effect of friction in the contact surface, and measurement error.

## Cracked Plate- Application to a compact tension specimen

A three dimensional FE model of a compact tension, C(T), specimen was created in ABAQUS. Due to symmetry, only a quarter of the C(T) specimen was modelled. The material model used was again aluminum alloy 2650. A highly refined mesh was generated in the vicinity of the crack tip region to ensure valid stress and strain data from the FE analysis. The model used eight-node hexahedral elements with reduced integration. A 25mm diameter punching tool with elastic-perfectly plastic material behaviour was again modelled in this simulation.

FE analysis showed that the state of residual stress was highly dependent on the size as well as the position of the punching tool. Attention was focussed on the stress component normal to the crack-plane, (33, as this will be the component which provides the crack driving force. To investigate the effect of size and the position of the punching tool a FE parametric study was carried out using three different tool diameters 25mm, 15mm and 7.5mm. To specify the position of the punching tool, a dimensionless parameter (x/R) was defined using the relative position of the punching tool and the crack in the specimen, where x is the distance between the centre of the punching tool and the crack-tip, and R is the radius of the punching tool. This is indicated in Fig. 5(a). The crack length, a, was 25mm with a/W=0.5. As the punching tool was moved, its axis remained along the crack line to maintain symmetry.

The three punching tools were applied at four different positions on the specimen. Figure 5(b) shows the relative positions of the punching tools with respect to the crack tip used in the FE simulations. The first position corresponded to x/R=1.0, which meant the edge of the punching tool was tangential to the crack front. The punching tool was then moved towards the crack-tip and positioned at x/R=0.75, 0.5 and 0.

Figure 5. (a), Parametric study of the punch position, (b) Four different position of punch

A sample of the results from the FE analysis is shown in Fig. 6(a), where distributions of the stress normal to the crack, (33, along a path in the centre of the specimen, starting from the crack tip, are illustrated for the three different punch sizes. The largest region of tensile residual stress was produced by the 25mm punch for x/R=1.0. The residual stress field for other x/R locations lead to similar patterns and suggested that the 25mm punching tool produced the greatest region of tensile residual stress ahead of the crack. The tensile residual stress field covered a large envelope throughout the thickness of the specimen in the case of using 25mm diameter punching tool. In the case of the 15mm punch both compressive and tensile residual stress ahead of the crack were produced. The 7.5mm diameter punching tool produced tensile residual stresses in the centre of the specimen to an extent equal to almost half of the thickness of the plate. The residual stress on the surface was compressive.

Figure 6. (a) Normal residual stress in the centre of the specimens (a) three different punch sizes (b) four different punching positions (b)

Fig. 6(b) indicates that the greatest tensile residual stress is introduced within the specimen when the punch is positioned tangential to the crack tip (x/R=1.0).

5. DISCUSSION AND CONCLUDING REMARKS

Local compression has been investigated as a method of introducing a well-defined residual stress field in semi-infinite, uncracked and cracked specimens. FEA was used to model the elastic indentation of the punching process in order to validate the simulations against known analytical solutions. Excellent agreement was found. The influence of remote boundaries on the elastic stress field was then studied and it was shown that they could modify the half-space stresses by up to approximately 40%.

FE analyses were then extended to predict the residual stress fields remaining after elasto-plastic punching a half-space, an uncracked plate and a cracked plate (a C(T) specimen). It was shown that application of LC on a semi-infinite body produced a tensile in-plane residual stress near the surface and a compressive stress deeper inside the body. LC on a 15mm thick plate resulted in a compressive residual stress through the complete thickness of the plate. This was confirmed by experimental measurements. The level of compressive residual stress measured was less than FE results, although the experimental and numerical results exhibited similar trends. Possible reasons for this discrepancy were highlighted.

FE simulations of LC on a cracked specimen indicated that the resulting residual stress field was highly dependent on the diameter of the punch as well as its position relative to the crack-tip. Simulations demonstrated that full through thickness tensile residual stresses were achieved for a punch diameter greater than the specimen thickness. It was found that significant tensile residual stresses ahead of the crack tip could be obtained by a) positioning the punch tangent to the crack-tip and b) using a punch diameter equal to the ligament. Finally, and most importantly, it was observed that LC produced a tensile residual stress field in the cracked body in the region under the punch.

6. REFERENCES

[1]	Johnson K.L., Conact mechanics, Cambridge University Press, 1999.

[2]	Shield R.T., On the plastic flow of metals under conditions of axial symmetry, Proceedings Royal Society of London, Series A Maths & Phys, A233, 267, 1955.

[3]	British standard, BS 7448: Part 2, Annex D, 1997.

[4]	Weld Fracture Test Standard (Proposed Annex to E1290), ASTM Revision 6, 1998.

[5]	Nepershin R.I., “The indentation of a flat punch into a rigid-plastic half-space”, Int. J. Appl. Maths. Mechs, Vol. 66, No. 1, pp. 135-140, 2002.

[6]	Harding J.W.and Sneddon I.N., The elastic stresses produced by the indentation of the plane surface of a semi-infinite elastic solid by a rigid punch, Cambridge philosophical society, 41, 1945.

[7]	Sneddon Ian N., Boussinesq’s problem for a flat-ended cylinder, Proc. Cambridge Philosophical society, 42, 1946.

[8]	Lee C.H., Kobayashi S., Elastoplastic analysis of plastic-strain and axisymmetric flat punch indentation by the finite element method, International journal of mechanical science, Vol. 12, pp. 349-370, 1970.

[9]	Almer J.D., Cohen J.B., and Winholtz R.A., “The effect of residual macrostresses and microstressses on fatigue crack propagation”, Metallurgical and Materials Transactions A, Vol. 29, 2127, 1998.

[10]	Ogeman R., “Coining Residual Stresses in Aluminium Ship Structures: Experiments and FE- simulations”, Dissertation, School of Mechanical and Vehicular Engineering, Department of Marine Structural, Sweden, 1993.

[11]	Meith W.A., Panontin T.L., Hill M.R., “ Analytical and experimental study of fracture in bend specimens subjected to local compression” Fatigue and Fracture Mechanics: 33th Volume, ASTM STP 1417, 2002.

[12]	Leggatt, R H . Smith, D J. Smith S D. and Faure F, Development and experimental

validation of the deep hole method for residual stress measurement, J.

Strain Analysis, 1996, Vol 31, No 3, pp 177-186

[13]	ABAQUS/Standard and viewer Version 6.2,Hibbit Karlsson and Sorenson, 1080 Main Street, Pawtucket, RI 02860-4847, USA, 2001.

[14]	Garcia-Granada A.A., PhD thesis, University of Bristol, October 2000.

# Text boxes

(a)

(b)

(a)

(b)

Figure 3. Residual stress distribution along the axis of symmetry of half-space following LC

Figure 4. In-plane residual stresses through the thickness of the plate

(b)

2R

(a)

(a)

(b)