## Slide 1
Emulsion Copolymerization of Silicone Oil Modified Vinyl Acetate-Butyl Acrylate Nanocomposite with Aid of Ultrasonic Technic for Use in Paint
Golamhossein Zohuria,*,Pedram Hosseinpourb, Mehran Gholamic a, b Department of Chemistry, Faculty of Sci e, Ferdowsi University of Mashhad, Mashhad, Iran c Samed Industrial and Manufacturing Co., Mashhad, Iran zohuri@um.ac.ir
Introduction
Methods
Results and Discussion
Conclusion
References
Inorganic-organic nanocomposite systems latex particles were synthesis using emulsion copolymerization systems. Silicone oil which has excellent heat, weather, and UV resistance and high hydrophobicity was used as modifier for the polymerization. Dynamic light scattering (DLS) diagrams showed that the average diameters of VAc-BA latex and nanocomposite particle size were about 170 and 180 nm, respectively. DSC data and Viscosity of the latex were increased with addition of the silicone oil. Using ultrasonic method for dispersion of the oil in the water and surfactants media caused fully and uniform dispersion. The average diameter of silicone oil particle dispersed was about 50 nm. Fortunately, the prepared paint of the latex preformed have excellent wet scrub resistance. Synthesis of polymer-silica nanocomposites using coupling agent [1], silicone modified acrylate emulsion [2], and modification of nano-SiO2 by oleic acid [3] are examples of preparation
The silicone oil was dispersed into distilled water and surfactants with the aid of ultrasonic method. The semi- continuous emulsion copolymerization technology was used to synthesis the silicone oil modified VAc-BA emulsion polymer. Emulsion polymerization were carried out in a 1 L glass reactor with a mechanical stirrer, reflux condenser, and a temperature controller at 72 °C for about 5 h. Some amount of total monomers (10%) were charged at the beginning of the polymerization, and the remaining mono-mers were added under monomer-starved condition to the end of the polymerization.
1- Barari M., Sharifi- Sanjani N., J. Appl. Polym. Sci, 2008, 110, 929-937. 2- Jiang B., Hu S., Liu Y., Wang M., Adv. Materials Research, 2011, 168- 170, 2055-2059. 3- Mahdavian A., Ashjari M., BayatMakoo A., Europ. Polym. J, 2007, 43, 336-344. 4- Khanjani J., Zohuri G.H., Gholami M., Shojaei B., Dalir R., J. of adhesion, 2014, 90, 174-194. 5- H. Yildirim Erbil, Polymer, 1996, 37, 5483-5491.
inorganic-organic nanocomposite.
DLS diagrams of the silicone oil dispersed is shown in Figure 1A and the average diameter was about 50 nm with 100% number. DLS diagrams of VAc-BA latex and nanocomposite are shown in Figure 1B and 1C and average diameters were about 170 and 180 nm with 100% number, respectively. The increase in particle size confirms the formation of nanocomposite particles. DSC thermogrames showed that Tg was increased in present of the silicone oil.
Water base nanocomposite was prepared via semicontinuous emulsion copolymerization. Silicone oil that was dispersed in water and surfactants with aid of ultrasonic increased Tg and viscosity of the obtained latex. The paint that prepared from
The viscosity of the latex also was increased when the silicone oil was added to the formula. The properties of Vac-BA and nanocomposite latex were listed in Table 1.
code | Viscosity (cp) | Tg ( ̊C ) | Particle size (nm) (PdI) | Solid content (%) | Conversion (%) | Mv (×105)
VB82-3 | 247 | 18.63 | 172(0.215) | 48.65 | 94 | 0.93
VB82-O,2 (with oil) | 420 | 27.10 | 184(0.212) | 50.31 | 95 | 1.43
Table 1 Properties of VAc-BA and nanocomposite latex.
The methods of solid content and conversion measurement are as reference 4 and the method for calculation of average viscosity molecular weight is as reference 5.
Based on ISO 11998, wet scrub resistant of paint was decreased from 0.43 to 0.14 mg.cm-2 with addition of the silicone oil.
VB82-O,2 latex improved wet scrub resistance to about 3 times.
(A) (B) (C)
Figure 1 DLS diagrams of (A) the silicone oil dispersed, (B) VAc-BA latex and, (C) nanocomposite.
Notes: <number>